1.Place in a burnout furnace and preheat to approximately 1000 centigrade for 1-2 hours8.Pour the creamy mixture into the prepared ring containing the wax patternManipulation of Investment Material5.Using a mixing spatula, mix for 15-30 seconds until all of the powder is mixed with the liquid3.Using a vacuum mixing machine, vacuum mix for 30 -60 seconds4.leaving it empty to receive the casting alloy.Working time is 2-4 minutes.6.7.9.
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