Properties of Nanomaterials:Nanomaterials have the structural features in between of those of atoms and thebulk materials.(12): Fluorescence emission of (CdSe) ZnS quantum dots of various sizes andabsorption spectra of various sizes and shapes of gold nanoparticlesThe optical properties of nanomaterials depend on parameters such as feature size,shape, surface characteristics, and other variables including doping and interactionwith the surrounding environment or other nanostructures.Due to their small dimensions, nanomaterials have extremely large surface area tovolume ratio, which makes a large to be the surface or interfacial atoms, resultingin more "surface" dependent material properties. Especially when the sizes ofnanomaterials are comparable to length, the entire material will be affected by the30surface properties of nanomaterials. This in turn may enhance or modify theproperties of the bulk materials. For example, metallic nanoparticles can be used asvery active catalysts. Chemical sensors from nanoparticles and nanowiresenhanced the sensitivity and sensor selectivity. The nanometer feature sizes ofnanomaterials also have spatial confinement effect on the materials, which bringthe quantum effects. The energy band structure and charge carrier density in the materials can bemodified quite differently from their bulk and in turn will modify the electronicand optical properties of the materials. For example, lasers and light emittingdiodes (LED) from both of the quantum dots and quantum wires are verypromising in the future optoelections. High density information storage usingquantum dot devices is also a fast developing area. Reduced imperfections are alsoan important factor in determination of the properties of the nanomaterials. Nanosturctures and Nanomaterials favors of a self-purification process in that theimpurities and intrinsic material defects will move to near the surface upon thermalannealing. This increased materials perfection affects the properties ofnanomaterials. For example, the chemical stability for certain nanomaterials maybe enhanced, the mechanical properties of nanomaterials will be better than thebulk materials. The superior mechanical properties of carbon nanotubes are wellknown. Due to their nanometer size, nanomaterials are already known to havemany novel properties. Many novel applications of the nanomaterials rose fromthese novel properties have also been proposed. Optical properties:One of the most fascinating and useful aspects of nanomaterials is their opticalproperties. Applications based on optical properties of nanomaterials includeoptical detector, laser, sensor, imaging, phosphor, display, solar cell,In this class of material, polymers filled with silicate platelets exhibit the bestmechanical properties and are of the greatest economic relevance. The larger theparticles of the filler or agglomerates, the poorer are the properties obtained. Although, potentially, the best composites are those filled with nanofibers ornanotubes, experience teaches that sometimes such composites have the leastductility. On the other hand, by using carbon nanotubes it is possible to producecomposite fibers with extremely high strength and strain at rupture. Among themost exciting nanocomposites are the polymer- ceramic nanocomposites, wherethe ceramic phase is platelet-shaped. This type of composite is preferred in nature,and is found in the structure of bones, where it consists of crystallized mineralplatelets of a few nanometers thickness that are bound together with collagen as thematrix. Composites consisting of a polymer matrix and defoliated phyllosilicatesexhibit excellent mechanical and thermal properties. Magnetic properties:Bulk gold and Pt are non-magnetic, but at the nano size they are magnetic. Surfaceatoms are not only different to bulk atoms, but they can also be modified byinteraction with other chemical species, that is, by capping the nanoparticles. Thisphenomenon opens the possibility to modify the physical properties of thenanoparticles by capping them with appropriate molecules. Actually, it should bepossible that non-ferromagnetic bulk materials exhibit ferromagnetic-like behaviorwhen prepared in nano range. One can obtain magnetic nanoparticles of Pd, Pt andthe surprising case of Au (that is diamagnetic in bulk) from non-magnetic bulkmaterials. In the case of Pt and Pd, the ferromagnetism arises from the structuralchanges associated with size effects.Disadvantages of Nanomaterials:? Instability of the particles Retaining the active metal nanoparticles ishighly challenging, as the kinetics associated with nanomaterials is rapid. In order to retainnanosize of particles, they are encapsulated in some other matrix. Nanomaterials are thermodynamically metastable and lie in the region ofhigh-energy local-minima. Hence they are prone to attack and undergotransformation. These include poor corrosion resistance, high solubility, andphase change of nanomaterials. This leads to deterioration in properties andretaining the structure becomes challenging. Fine metal particles act as strong explosives owing to their high surface areacoming in direct contact with oxygen. Their exothermic combustion caneasily cause explosion. ? Impurity - Because nanoparticles are highly reactive, they inherently interactwith impurities as well. In addition, encapsulation of nanoparticles becomesnecessary when they are synthesized in a solution (chemical route). Thestabilization of nanoparticles occurs because of a non-reactive speciesengulfing the reactive nano-entities. Thereby, these secondary impuritiesbecome a part of the synthesized nanoparticles, and synthesis of pure Electrical Properties:Electrical Properties of Nanoparticles" discuss about fundamentals of electricalconductivity in nanotubes and nanorods, carbon nanotubes, photoconductivity ofnanorods, electrical conductivity of nanocomposites.As the nanotubes have different lengths, then with increasing protrusionof the fiber bundle an increasing number of carbon nanotubes will touch thesurface of the mercury droplet and contribute to the electrical current transport.photocatalysis, photoelectrochemistry and biomedicineCdSe Nanoparticles2.3nm5.5nm1.0-0.8-Gold Nanoparticles06-15nm nanospheres30nm nanospheres04-2.5AR nanorods-4.5AR nanorods7.5AR nanorods02-Photo Felice Frankel0.0-400500600 700 800 900 1000 1100 1200 1300Wavelength (nm)Fig.This is mainly due to the nanometer size of the materials which render them: (i)large fraction of surface atoms; (ii) high surface energy; (iii) spatial confinement;(iv) reduced imperfections, which do not exist in the corresponding bulk materials.As the lengths and orientations ofthe carbon nanotubes are different, they touch the surface of the mercury atdifferent times, which provides two sets of information: (i) the influence of carbonnanotube length on the resistance; and (ii) the resistances of the differentnanotubes.While most microstructured materials have similar properties to thecorresponding bulk materials, the properties of materials with nanometerdimensions are significantly different from those of atoms and bulks materials.One interesting method whichcan be used to demonstrate the steps in conductance is the mechanical thinning of ananowire and measurement of the electrical current at a constant applied voltage.The important point here is that, with decreasing diameter of the wire, the numberof electron wave modes contributing to the electrical conductivity is becomingincreasingly smaller by well-defined quantized steps.(13): Electrical behavior of naotubesIn electrically conducting carbon nanotubes, only one electron wave mode isobserved which transport the electrical current.However, when an anisotropy is added to thenanoparticle, such as growth of nanorods, the optical properties of the nanoparticleschange dramatically.With the CdSe semiconductor nanoparticles, a simple change in sizealters the optical properties of the nanoparticles.When metal nanoparticles areenlarged, their optical properties change only slightly as observed for the differentsamples of gold nanospheres.(12)Exemplifies the difference in the optical properties of metal and semiconductornanoparticles.Likewise, shape canhave dramatic influence on optical properties of metal nanostructures.MetalSemiconductorGraphiteFig.Fig.