8.2 Evaluation of the cleaning process reveal the mechanismFor research purposes, the measurements do not need to be quick, easy to handle and non-invasive.Visual inspection is an off-line method and can range from ordinary photosto follow the course of cleaning, but also together with dyes for specific elements andmicroscopic techniques to enhance the details and resolution.Using Scanning electronmicroscopy (SEM) structural changes of the fouling, such as the swelling of the proteindeposit, can be revealed.By monitoringand analyzing the effluent during cleaning over time, important information is obtained; suchas when the protein and mineral content is released in comparison to each other and to thecurrent parameters used for the cleaning process.UV-absorbance can be used in cleaning studies to investigate the effluent concentration ofproteins [84].The content of the mineral deposit could be obtained in using aSEM-EDX, giving the elemental composition in a certain area of the sample [111].Following the fouling removal (and buildup) with a direct online measurement with time on asurface inside a process plant is difficult to do on an industrial scale.It is also possible to measure the protein content by measuring the chemicaloxygen demand (COD) [5, 56] or the Kjeldahl method [31, 49-51].Downsizing theequipment to a smaller pilot plant is many times used for research purposes, but still has notgiven the obvious methods to online and on site follow the changes of the fouling.From effluent analysis, the originalcomposition of the fouling can be determined, but without any spatial information.Since it'scommon to foul the surfaces in a closed system, it is difficult to a priori visualize anddetermine the microstructure.Thenoninvasive effluent analysis are common in pilot scale cleaning studies [107].The equipment can be dismantled and prepared at different stages and for differenttype of analyses.An analysis of the effluentcan only tell when there is nothing left leaving the equipment, but cannot validate that thesurface is clean.The above mentioned methods are the same as discussed in chapter 4 under foulingcharacterization.