A better understanding of the physics of entropygeneration at multiple length scales (micro--tomacroscale) during fatigue damage may providemore insight into the stochastic nature of fatiguefailure.An accurate evaluation of entropy generation at multiple length scalesmight therefore shed more light on the physics offatigue crack initiation.Since entropy generation is an additive function, the total entropy generation can be presentedas the sum of entropy changes associated with thematerial and process at corresponding scale levels:dStot m = + dS icro dSmeso + dSmacro (2)where Stot = total entropy generation of the systemunder study; Smicro = entropy generation at microscale; Smeso = entropy generation at mesoscale; andSmacro = entropy at macroscale.As a consequence ofthe ongoing cyclic slip process, the Persistent SlipBands (PSBs) evolve and interact with high-angleGrain Boundaries (GBs), the result of which leadsto dislocation pile-ups, static extrusions in theform of ledges/steps at the GB, stress concentration, and ultimately crack initiation.We present entropy generation of dislocationactivities to find answers for some fundamental questions: whether fatigue damage is a submartingale or strictly increasing function withtime; whether entropy, instead of its counterpart,energy function, provides additional insights intoour understanding of fatigue damage evolution;and whether entropy can be used in a fundamentalway to predict the evolution of damage enablingfatigue life predictions.Regardingfatigue, damage may be defined as a reduction in theYoung's modulus, as a cumulative number of cyclesratio, as a reduction of load-carrying capacity, ascrack length, or as released strain energy (Amiri &Modarres 2014.) In this paper, we consider fatiguedamage as slip irreversibilities that exist in a materialand accumulate during fatigue loading.3 Entropy as damage metric3.1 Various forms of degradationThe Degradation-Entropy Generation (DEG)theorem developed by Bryant et al. (2008) statesthat the rate of degradation is related to the irreversible entropy generations by the underlying dissipative physical processes that degrade materials.That is, a structural transformation takesplace in the dislocation ensemble upon crack initiation such that randomly-distributed-dislocationdensity reduces due to self-organization and theformation of the patterned planar-dislocationwall structure or microcracks.This criterion known asLyapunov's theory of stability may provide a crackinitiation criterion based on the entropy of thesystem by defining a control parameter x whichis changing from equilibrium state A to equilibrium state B. Control parameter x is defined in thecontext of statistical thermodynamics by Jarzynski (2011).However, the formation of the patterned planar-dislocation-wall structures at microscale and submicron may be considered as theconfiguration entropy that decreases and results inincreased orderliness of the system, i.e. dSmicro0.Ostoja-Starzewski & Malyarenko(2014) use the Doob-Meyer decomposition whichsays that under mild technical conditions any submartingale is the sum of a martingale (M) and anincreasing process (G).This concept has been stablised within the contextof statistical mechanics which indicated that thatthe deterministic nature of non-decreasing dissipation function is the average manifestation of astatistically fluctuating dissipation on very smallscales.As mentioned above, in calculation of entropy, it is of paramount importance toconsider behavior of entropy evolution at multiplelength scales, because entropy generation at smallscales is a stochastic phenomenon with possibledeviation from the second law of thermodynamics.Amiri & Modarres (2014) haveinvoked this hypothesis and have shown that therate of damage in various processes such as fatigue,wear, corrosion, radiation damage and creep can beevaluated based on the rate of entropy generation.Stewart et al. (2006) employednon-equilibrium thermodynamics theory to predictthe initiation of dynamic recrystallisation (DRX)for nickel and steels.3.3 Fatigue crack initiationAs mentioned earlier, it is widely accepted thatstrain localization due to increasing dislocationdensity during cyclic forward and reverse loading is a precursor to fatigue crack initiation.Equation (2) suggests that even if bulk stress andstrain are in the elastic range, the vicinity of inherent micro defects deformation can be locally plastic.From definitionof Gibbs free energy and its relation to entropy ofthe system G = H-TS, where H is enthalpy, T istemperature and S is entropy, we will derive the4104necessary entropic condition for crack initiationbased on instability criterion of the system:120 2 ?However, the decrease of entropy and increase oforderliness at microscale is compensated by theentropy increase at the mesoscale due to the formation and propagation of cracks, i.e. dSmeso0.Ni is thefatigue nucleation life associated with virtual cracklength a. Mathematically, to maximize the Gibbsfree energy, one can write:d Gda Ni?The in situ neutron diffraction study by Huanget al. (2010) states that dislocation self-organizationarises possibly during the formation of a microcrack.2.1 Entropy balance at multiple length scalesLet us confine our discussion to length scale thatspans from micro to macro.In an open system capable of exchanging heatand matter with its surroundings the change of thetotal entropy, dS consists of sum of two parts:dS = d S ( ) e i +d S ( ) d S ( )i ; 0 (1)where d(e)S is the entropy exchange with the surroundings (or reversible entropy change) and d(i)S is the entropy generation within the system (orirreversible entropy change).This suggests that even if bulk material undergoes a reversible process, at lower scales it mightexperience irreversibilities that are not observed atcontinuum level.This theorem states that there is one-to-one correspondence between the rate of entropy generation and the rate of degradation relating to eachother through a scaling factor called degradationcoefficient.Asoutlined in the previous section, the entropy generation is a submartingale meaning that at smallscales the entropy generation can become negativethat gives rise to behavior not seen under the restriction of the conventional second law of thermodynamics.As discussed byMughrabi (2009), the mechanisms of cyclic microplasticity, based on the glide of dislocations, areresponsible for the fatigue phenomena.In fact,cyclic slip irreversibilities in a microstructural senseoccur not only at the surface but also in the bulkat the dislocation scale which contribute to surfacefatigue damage.Employing non-equilibrium thermodynamics, we may develop the necessary formulations for evaluations of entropy generation duringfatigue damage.The rate of entropy generation due to dislocations activities can be expressedas (Huang et al. 2009):dS Gb dT = ++ ?As stated earlier, ifa nonequilibrium stationary system loses its stability, the excess entropy should satisfy the inequalityin (7).= constants.Therefore, d??????12?2 ??2).2).? ) = ??